## Slide 1
Institute of Physics, Chinese Academy of Sciences
Theory of high Tc nickelate superconductors &
Possible upper limit of Tc for unconventional superconductivity
Yi-feng Yang
Collaborators:
Qiong Qin, Jiangfan Wang, Yingying Cao
Guang-Ming Zhang, Fu-Chun Zhang
Refs: npj Quantum Mater. 10, 13 (2025); The Innov. Mater. 2, 100102 (2024); CPL 42, 017301 (2025).
PRB 108, L140504 (2023);108, L201108(2023); 109, L081105 (2024); 110, 104507 (2024); 111, 014512 (2025).

## Slide 2
Key questions on high Tc nickelates
q What is the minimal effective model?
q What is the pairing mechanism & pairing symmetry?
q What determines the maximum Tc?
q Why is Tc reduced from bilayer to trilayer nickelates?
q How to explain the non-Fermi liquid normal state?
q What can we learn from nickelates?

## Slide 3
DFT+DMFT: Flat bands promoted by Hund coupling
Y. Cao & YF, PRB 109, L081105 (2024); arXiv:2307.06806
Orbital-dependent mass enhancement due to Hund
Flat dz2 bands (hybridized with) dispersive dx2-y2 bands
Local dz2 moment with strong interlayer superexchange
XJ Zhou et al.
Interlayer valence bonds & hybridization & Hund physics

## Slide 4
Minimal t-V-J model, two-component theory of SC, and maximum Tc
Two-component composite pairing
YF, G-M Zhang, F-C Zhang, PRB 108, L201108 (2023)
Minimal t-V-J model
Q. Qin & YF, PRB 108, L140504 (2023)
Auxiliary-field MC simulations
(Moderate U, no 𝛄 pocket)
dz2 for pairing interaction, dx2-y2 for phase coherence
s+- gap with nodes or minima along zone diagonal on 𝜶/𝜷
Maximum Tc≈0.04-0.05J gives 70-90 K for J~150 meV (RIXS/INS); promoted by uniaxial pressure
Reduced Tc in thin films, possibly due to the reduced J

## Slide 5
Highly asymmetric Tc curve and non-Fermi liquid upon hole doping
Critical hole doping (large U) & highly asymmetric Tc curve
Pseudogap & strange metallicity also obtained above Tc
How about moderate U? (work in progress)
J. Wang & YF, PRB 111, 014512 (2025).
M Wang et al.
Schwinger boson approach to treat both SC and interlayer valence bonds (large U)

## Slide 6
Kondo effect and Fano interference
dz2
narrow bands
Possible Fano interfore in quasiparticle tunneling
like in heavy fermion systems
YF, Phys. Rev. B 79, 241107(R) (2009)
dx2-y2
broad bands
YF, CPL 42, 017301 (2025).

## Slide 7
Suppressed Andreev reflection
Andreev reflection is suppressed for weak interlayer hopping due to Gutzwiller constraint
Systematic evolution under pressure or doping tuning
𝜸: full gap (+);
𝜶(+)/𝜷(-): s-wave gap with nodes/minima along zone diagonal
Interlayer hopping scaling factor
for small t⊥ self-doped hoels on dz2
∝
How to compare with experiments by HH Wen et al. & HQ Yuan et al.?
YF, CPL 42, 017301 (2025).

## Slide 8
Bilayer La3Ni2O7:
Trilayer La4Ni3O10:
Q. Qin, J. Wang, & YF, The Innov. Mater. 2, 100102 (2024)
Frustrated superconductivity in trilayer nickelate
Strong interlayer SC fluctuations
s± wave pairing with gap nodes or minima
along the zone diagonal direction
Monte Carlo simulations of the pairing fields

## Slide 9
Intrinsic reduction of the maximum Tc
bilayer: max Tc～70-90 K vs 80 K
trilayer: max Tc～30-50 K vs 30 (39?) K
Taking J～150 meV ?
Maximum Tc/J ~ 0.04-0.05 for bilayer
Maximum Tc/J ~ 0.02-0.03 for trilayer
RIXS & INS
Contrary to cuprates where Tc is of record high in trilayer structures.
Maybe further reduced by layer imbalance & smaller J?
DL Feng et al.
M Wang et al.
Q. Qin, J. Wang, & YF, The Innov. Mater. 2, 100102 (2024)

## Slide 10
Decomposition of interlayer pairing superconductivity (L≥4)
YF, Phys. Rev. B 110, 104507 (2024)
Multilayer t-V-J model:
Decompose into bilayer blocks (plus one trilayer for odd L)
Maximum Tc possibly determined by the blayer blocks
Possible high Tc under valence tuning
To minimize the free energy

## Slide 11
Emergent superconducting stripes in two-orbital superconductors
Q. Qin & YF, arXiv:2508.14632 (2025)

## Slide 12
What can we learn from nickelates?

## Slide 13
Momentum-space vs. real-space pairing

## Slide 14
Static auxiliary-field Monte Carlo

## Slide 15
Can we further improve the maximum Tc?
Q. Qin & YF, npj Quantum Mater. 10, 13 (2025)
maximum Tc ~ 0.04-0.07 J
Tc=300 K requires J > 400-700 meV (@ optimal t/J)
Infinite-layer nickelates could host higher Tc ? (new 40 K samples? or pressure tuning?)
Most iron-based SC (except 11 & 1111) also has low ratios, why?
RNiO2
X
La3Ni2O7 ?
X

## Slide 17
Revisit the infinite-layer nickelates

## Slide 18
Revisit the cuprate superconductors
Q. Qin & YF, npj Quantum Mater. 10, 13 (2025)

## Slide 19
Revisit the iron-based superconductors
Q. Qin & YF, npj Quantum Mater. 10, 13 (2025)

## Slide 20
Can we achieve the room-temperature SC?

## Slide 21
Materials design from real-space pairing

## Slide 22
Summary
q The minimal effective model: Two-orbital t-V-J model
q Hund: important for flatband
q Pairing: Two-component theory, anisotropic s±-wave
q Maximum Tc: ~0.04-0.05 J (bilayer); 0.02-0.03 J (trilayer)
q Non-Fermi liquid normal state: Near optimal doping
q dz2 metallization: crucial (Jiangfan Wang’s talk)
Maximum Tc ~ 0.04-0.07 J
Real-space route for materials design of more high-Tc superconductors